## Slide 1: Session 5 – CIPS Inputs and Training Exercise
VERA Users Group Training
Oak Ridge National Laboratory 2/14/2019

## Slide 2: Contents
VERA CIPS Analysis Overview
CRUD/Chemistry input overview
CIPS exercise with SMR cycle
  Cycle with enough CRUD/boron to show CIPS
  CRUD shuffling and cleaning
    Cycle with crud with restart file
    Cycle with crud shuffle
CRUD capabilities in VERAView
  Postprocessing for AO deviation and pin power differences using VERAView
  Look at whole-core crud and crud shuffle

## Slide 3: Disclosures
Mamba is still under development
Milestones this year for
  Mass balance
  Calibration
  Documentation
CILC tools are still under development
  Milestone to improve usability
  Officially outline and document updated CILC capability
This give you the chance to be involved and help form the tools

## Slide 4: Crud Deposition in Reactors
Crud is the buildup of particulate and dissolved metals and metal oxides on the fuel rod surfaces and is problematic because:
  It reduces heat transfer
  It accelerates cladding oxidation/corrosion
  It provides a structure for the hideout and precipitation of chemical species
Crud Induced Power Shift (CIPS) is the neutronic feedback to the precipitation of significant amounts of boron containing chemical species
Crud deposition negatively affects the operation and efficiency of reactors

## Slide 5: Root Cause of CIPS
CIPS is a complex thermal-chemical-neutronic interaction
EPRI. (1997). Rootcause Investigation of Axial Power Offset Anomaly.
LiBO2, Li2BO7, and Li2B4O7

## Slide 6: Effect of CIPS on Reactors
CIPS leads to an imbalance in the core power distribution and decreases operation margin
6

## Slide 7: VERA CRUD Analysis Overview
Captures coupled neutronics, thermal-hydraulic, source term, and clad chemistry
Able to run all physics or subsets for more flexibility
Adds input from CFD to capture rod surface distributions
Single capability to handle CIPS and CILC

## Slide 8: Why use CRUD physics in VERA? CIPS Analysis of Watts Bar 1 Cycle 7
VERA has been used to perform CIPS analysis of
Caveat!
  MAMBA is not yet predictive and is still under active development.
Look at detector response for these points in time

## Slide 9: WB1C7 Detector Response – Before Shutdown
VERA without CRUD
VERA with CRUD

## Slide 10: WB1C7 Detector Response – After Restart
VERA without CRUD
VERA with CRUD

## Slide 11: WB1C7 Cycle Average Error Distribution
VERA without CRUD
VERA with CRUD
The previous caveat still applies.
But if we can match the CIPS phenomena, then it is possible to predict CIPS phenomena if MAMBA can get the right amount of CRUD and borate in the right places.

## Slide 12: Manual Crud/Chemistry Input Overview
[STATE]
crud on !Enables crud/chemistry physics package
[STATE] deplete EFPD 12; cool_chem 35E-6 2.2 0.19 2.120 1.8
[STATE] deplete EFPD 25; cool_chem 35E-6 2.2 0.19 2.194 1.7
[STATE] deplete EFPD 50; cool_chem 35E-6 2.2 0.19 2.193 1.7
[STATE] deplete EFPD 75; cool_chem 35E-6 2.2 0.19 2.890 1.7
[STATE] deplete EFPD 100; cool_chem 35E-6 2.2 0.19 2.688 1.7
[STATE] deplete EFPD 125; cool_chem 35E-6 2.2 0.19 2.890 1.7
[STATE] deplete EFPD 150; cool_chem 35E-6 2.2 0.19 2.688 1.7
Hydrogen Lithium Ni_sol Ni_par Fe_sol
(kg/m^3) (ppm) (ppb) (ppb) (ppb)
[STATE] deplete EFPD 100; ni_p 2.890; ni_s 0.19
[STATE] deplete EFPD 125
ni_p 2.720
ni_s 0.19
Moving towards individually named cards in each [STATE]
**What do you think?

## Slide 13: CIPS Exercise with SMR Cycle
CAVEAT!
These models are optimized for speed and to show explicit CRUD effects. Many of the values for the inputs in these models are non-normal!
Make sure you are in your home directory
  cd
Copy session5 files to your home directory
cp –r /projects/vera-users-grp/training/session5 .
Move into the session5/cips_smr directory
cd session5/cips_smr

## Slide 14: CIPS Exercise with SMR Cycle
  Open cips_smr.inp and add/change the following inputs:
  Save the chanes to the file and exit
  Execute VERA with CRUD physics package
  verarun cips_smr.inp
[STATE] !First STATE block needs crud flag
crud on
cool_chem 35E-6 2.2 0.19 3.5 1.8
[STATE] !Last STATE block needs to write restart file
deplete GWDMT 0.1 <1.0..9.0x2> ! big steps for speed (<=1 GWDMT normally)
op_date 2019/2/14
restart_write cips_smr.res EOC
[Assembly]
grid MID zirc4 3.810 875 / loss= 0.9 blockage= 0.5
[langtrav@lemhi1 results]$ verarun cips_smr.inp
[verarun] submitted job id=9730, dir=/home/langtrav/training/results
Optional grid parameters
loss defines the loss coefficient for the grid
blockage enables YHL grid enhancement model and defines blockage coefficient
Restart_filename NAME_for_statepoint

## Slide 15: CRUD Shuffling and Cleaning Exercise
Shuffles assemblies with crud carryover after cleaning
Restart file contains crud mass for every surface on every rod at EOC
Allow for the optimization of ultrasonic cleaning between cycles
Seabrook EOC 4
Seabrook BOC 5

## Slide 16: CRUD Shuffle Exercise
CAVEAT!
These models are optimized for speed and to show explicit CRUD effects. Many of the values for the inputs in these models are non-normal!
Make sure you are in your home directory
  cd ~/session5/shuffle/

## Slide 17: CRUD Shuffling and Cleaning Input
Open shuffle.inp and add/change the following inputs:
[STATE]
restart_shuffle ../cips_smr/cips_smr.res EOC
shuffle_label
+ P-3 N-2 K-2
N-6 N-1 N-3 +
K-3 M-3 N-3
P-2 +
crud_cleaning
- 0.6 - -
0.6 - 0.6 -
- 0.6 -
- -
crud_removal 0.1
[CORE]
cycle 2
op_date 2019/03/14
map of assemblies with
individual crud cleaning
fractions applied
each entry is fraction
of crud thickness removed
generic cleaning applied
to all assemblies
map of shuffled
assemblies from prior
depleted cycles
path-to-restart-file restart state name
date must be later than op_date on restart file
**What do you think?

## Slide 18: CIPS Capabilities in VERAView
Learn to:
  Open and manage multiple files
  Create and visualize a difference dataset (AO and pin_powers)

## Slide 19: Thank You!

## Slide 20: Extra Slides